## Slide 1: ISAC CASE STUDY
SPRAY DRIED DRUG LOADED POLYMERIC MICROPARTICLES
ISAC_CS_01

## Slide 2: Spray Dried Drug Loaded Polymeric Microparticles
An Atomic Force Microscopy (AFM) Case Study

## Slide 3: POLYMERIC MICROSPHERES FOR DRUG DELIVERY
Spray-dried polymeric microspheres have been investigated for use as a controlled release vehicle for active pharmaceutical ingredient (API) administration by intramuscular injection.
Combinations of biocompatible polymers can be deployed to balance a targeted release profile with appropriate API solubility and stability in-formulation.
One such example is a API/PLGA/PVP system (Meeus et al, 2012).
The surface characterisation of such systems is crucial in understanding how composition and environment affect physiochemical character and performance.

## Slide 4: SURFACE CHARACTERISATION METHODS
X-Ray Photoelectron Spectroscopy (XPS)
Elemental Composition
Chemical State Information
Time-of-Flight Secondary Ion Mass Spectrometry (ToF-SIMS)
Depth Profiling (layer-by-layer chemistry).
PVP - Red
PLGA - Green
(200×200µm2)
Scanning Electron Microscopy (SEM)
High magnification and resolution morphological and topographical characterisation
Sputter Time

## Slide 5: LIMITATIONS
X-Ray Photoelectron Spectroscopy (XPS) can quantify the elemental composition of the particle surfaces and provide information on the chemical state.
Time-of-Flight-Secondary Ion Mass Spectrometry (ToF-SIMS) can qualify the chemical composition and characterise fine changes on a nanometer resolution with depth.
  BUT these techniques cannot resolve the surface of an individual microparticle (size range <10µm)
Imaging with Scanning Electron Microscopy (SEM) provides visualisation on this scale.
  BUT offers no distinction of chemical constituents
None of these techniques make no mechanical assessment of the microspheres

## Slide 6: ATOMIC FORCE MICROSCOPY
Atomic Force Microscopy (AFM) is a high resolution scanning probe technique that allows visualisation of material surfaces and their topographical features with nanometre resolution, in addition to enabling surface physicochemical, mechanical, thermal or electrical properties to be measured.
SEM Image
AFM 3D Profile
Surface Characterisation down to the Nanoscale

## Slide 7: NANOSCALE VISUALISATION
AFM can identify the morphological differences between sample surfaces such as microsphere formulation variants.
API/PLGA/PVP Microspheres
10/75/15 (%wt)
Homogeneity
Uniformity
20/50/30 (%wt)
Morphology
Form, shape, structure
30/25/45 (%wt)
Topography
Distribution of features
Observe changes between formulations

## Slide 8: NANOMECHANICAL MAPPING
AFM offers the capacity to generate simultaneous ‘multi-channel’ data.
Sample topography can be complemented by simultaneous mapping and quantification of mechanical data including adhesion, stiffness etc.
Topographical variability distinguished from material differences i.e. API from polymer domains.
Microparticle Topography
Microparticle Stiffness
Different Materials
e.g. API / PLGA
Surface Depression

## Slide 9: ‘IN-SITU’ REAL TIME ANALYSIS
AFM allows observation of physical and chemical responses at the surface to formulation parameters, and real-time changes to the environment etc.
Height
Phase
Humidity 10%
Humidity 80%
E.g. AFM can characterise the surface rearrangement of constituent polymers due to a humidity increase.
Rearrangement and phase separation seen at the sample surface.
5µm x 5µm PLGA/PVP 40/60 wt

## Slide 10: SUMMARY
AFM is an invaluable tool in the characterisation of the surfaces of micro- and nano-scale materials such as single spray dried polymeric microparticle formulations
Nanomechanical data identified measurable phase differences representative of distinct API and polymer domains not resolved by other characterisation methods.
Real-time, ‘in-situ’ changes to single particle surfaces in response to environment observed.
AFM offers a unique capacity to complement broader chemical and visual analysis with nanometre resolution topographical, and simultaneous mechanical characterisation.
Insight from AFM develops understanding of formulation dynamics and responses that can be linked to performance and used in development

## Slide 11: REFERENCES
For more details on the work showcased in this case study see the following publications:
Nanoscale Surface Characterization and Miscibility Study of a Spray-Dried Injectable Polymeric Matrix Consisting of Poly(lactic-co-glycolic acid) and Polyvinylpyrrolidone. Joke Meeus, Xinyong Chen, David J. Scurr, Valeria Ciarnelli, Katie Amssoms, Clive J. Roberts,Martyn C. Davies, Guy Van Den Mooter. Journal of Pharm. Sci., 2012, 101, (9) 3473-3485
Surface Characteristics of Spray-Dried Microspheres Consisting of PLGA and PVP: Relating the Influence of Heat and Humidity to the Thermal Characteristics of These Polymers. Joke Meeus, David J. Scurr, Katie Amssoms, Martyn C. Davies, Clive J. Roberts and Guy Van den Mooter. Mol. Pharmaceutics 2013, 10, 3213−3224

## Slide 12: ADDITIONAL INFORMATION
If you wish to get in touch with us to discuss the information provided, raise a query/concern or provide feedback then please feel free to get in touch via any of the methods listed below:
  The Interface and Surface Analysis Centre (ISAC)
  Boots Science Building (C08)
  University Park
  Nottingham
  NG7 2RD
Telephone: +44(0)115 951 5046 / +44(0)115 645 3130
Email: isac@nottingham.ac.uk
Fax: +44 (0)115 846 7969
Website: www.nottingham.ac.uk/isac