NCMH PhDTutorial 2: Further Viscosity

Persistence length Lp and mass per unit length ML

Is a measure or chain flexibility - see the D2DBT7 lecture notes "Physical Biochemistry.    The mass per unit length ML depends on the saccharide repeat unit and the extent of branching.

The Bushin-Bohdanecky method1

This is one of the most popular methods for estimating chain persistence lengths particularly for semi-flexible polymers, and has been applied to range of polysaccharides from charged polysaccharides including xanthan2, sodium hyaluronate3 as well as galactomannans4 and certain neutral polysaccharides such as cereal -glucans5. In its simplest form, the Bohdanecky method (or Bushin-Bohdanecky method) involves plotting Mw2h13versus Mw12 and from the slope Lp/ML can be calculated using the following relation and tabulated values29 of the coefficient B0:

Mw2h13=Ah+B0F−132LpML−12Mw12

B0 is ~ 1.025 (ref. 30), the Flory-Fox ‘constant’ F is ~ 2.86 x 1023 mol-1 .

References

- Bohdanecky, M.  Macromolecules 1983, 16, 1483-1493 and Bushin, S.; Tsvetkov, V.; Lysenko, E.; Emelianov, V. Vysokomol Soedin 1981, 23A, 2494-2503

- Sato, T.; Norisuye, T.; Fujita, H. Macromolecules 1984, 17, 2696-2700.

- Mendichi, R.; Soltes, L.; Schierone, A. G. Biomacromolecules 2003, 4, 1805-1810.

- Patel, T. R.; Picout, D. R.; Ross-Murphy, S. B.; Harding, S. E. Biomacromolecules 2006, 7, 3513-3520.

- Gomez, C.; Navarro, A.; Manzanares, P.; Horta, A.; Carbonell, J. V. Carbohyd. Polym. 1997, 32, 7-15.

Question 1.

Describe in simple terms what you understand by (a) the mass per unit length ML of a polysaccharide and (b) the persistence length Lp.

Question 2.

Give a table of about 10 literature values for the mass per unit length ML and persistence lengths

Question 3.

The data in Table 1 describe the change in intrinsic viscosity with molecular weight for -irradiated xyloglucan samples.

Table 1. Hydrodynamic data for native and -irradiated xyloglucans in phosphate-chloride buffer, pH6.8, I=0.1

| Xyloglucan sample | [] (mL/g) | 10-4 x Mw (g/mol) |
| --- | --- | --- |
| XG-0 | 405 ± 35 | 70.0 ± 5.0 |
| XG-10 | 210 ± 10 | 27.0 ± 1.0 |
| XG-20 | 170 ± 10 | 15.8 ± 0.3 |
| XG-30 | 140 ± 10 | 12.7 ± 1.0 |
| XG-40 | 135 ± 5 | 9.7 ± 1.0 |
| XG-50 | 100 ± 5 | 6.0 ± 0.4 |
| XG-70 | 75 ± 5 | 4.5 ± 0.3 |

- Plot a Bushin-Bohdanecky plot (using ORIGIN)

- Evaluate the ratio Lp/ML from this plot.

- Using a literature value for ML of ~ 537 g mol-1 nm-1 (calculated from the Glc/Xyl/Gal ratio of 1:0.6:0.3) estimate the persistence length Lp.